Att. No. 1

ORDER DESCRIPTION

- Object of the contract

The subject of the order is the supply of semiconductors wafers listed below by name and quantity needed:

- InP SI 2” DSP     50 pieces

- InP SI 2” SSP     50 pieces

- InP SI 3” DSP     50 pieces

- InP SI 3” SSP     25 pieces

- InP SI 4” DSP     25 pieces

- Parameters

| Product name |  | Parametrer | Specification |
| --- | --- | --- | --- |
| 2” InP Semi Insulating Doped with Fe | Diameter 2” Thickness: 350±25 µm Diameter: 50.8±0.4 mm | Grade: | Prime, Epi-ready |
|  |  | Orientation: | (100)±0.3o |
|  |  | Primary Flat: | EJ (0-1-1) ±0.5o |
|  |  | Secondary Flat | EJ (0-11) ±0.5o |
|  |  | Resistivity: | >1E7 ohm cm |
|  |  | EPD (Average): | ≤10 000/cm2 max |
|  |  | Surface Finish: | DSP (double side polished) Side 1: Polished Side 2: Polished |
|  |  |  | SSP (single side polished) Side 1: Polished Side 2: Etched |
|  |  | Packaging: | ePAK, individual box, sealed with N2 in a moisture-stopping metallic foil bag, done in class 100 clean room. |
| Product name |  | Parametrer | Specification |
| 3” InP Semi Insulating Doped with Fe | Diameter 3” Thickness: 600±30 µm Diameter: 76.2±0.3 mm | Grade: | Prime, Epi-ready |
|  |  | Orientation: | (100)±0.3o |
|  |  | Primary Flat: | EJ (0-1-1) ±0.5o |
|  |  | Secondary Flat | EJ (0-11) ±0.5o |
|  |  | Resistivity: | >1E7 ohm cm |
|  |  | EPD (Average): | ≤10 000/cm2 max |
|  |  | Surface Finish: | DSP (double side polished) Side 1: Polished Side 2: Polished |
|  |  |  | SSP (single side polished) Side 1: Polished Side 2: Etched |
|  |  | Packaging: | ePAK, individual box, sealed with N2 in a moisture-stopping metallic foil bag, done in class 100 clean room. |
| Product name |  | Parametrer | Specification |
| 4” InP Semi Insulating Doped with Fe | Diameter 4” Thickness: 625±25 µm Diameter: 100±0.4 mm | Grade: | Prime, Epi-ready |
|  |  | Orientation: | (100)±0.3o |
|  |  | Primary Flat: | EJ (0-1-1) ±0.5o |
|  |  | Secondary Flat | EJ (0-11) ±0.5o |
|  |  | Resistivity: | >1E7 ohm cm |
|  |  | EPD (Average): | ≤10 000/cm2 max |
|  |  | Surface Finish: | DSP (double side polished) Side 1: Polished Side 2: Polished |
|  |  | Packaging: | ePAK, individual box, sealed with N2 in a moisture-stopping metallic foil bag, done in class 100 clean room. |