Attachment no. 1

ORDER DESCRIPTION

- Subject of the order

The subject of the order is the supply of gas listed below by name and quantity needed:

1. Arsine (AsH3)              1 bottle, 27 kg

- The scope of the subject of the contract

A detailed description of the subject of the contract is provided in section 5 of this document. The total price for the product specified in point 1 should include the total cost along with the packaging and delivery to the headquarters of the Ordering Party.

5. Parameters

| Product name | Parametrer | Specification |
| --- | --- | --- |
| Arsine (AsH3) | Grade: | ≥ 99.99995% |
|  | Valve Connection | Din 1 or Diss 632 Pneumatic |
|  | Impurities: Cadmium (Cd), Calcium (Ca), Chromium (Cr), Cobalt (Co), Copper (Cu), Gallium (Ga), Germanium (Ge), Lead (Pb), Magnesium (Mg), Molybdenum (Mo), Nickel (Ni), Silicon (Si), Sodium (Na), Tin (Sn), Zinc (Zn), | ≤10 ppbw |
|  | Impurities: Germane (GeH4), Silane (SiH4) | ≤50 ppbv |
|  | Impurities: Carbon Dioxide (CO2), Oxygen (O2) | ≤ 25 ppbv |
|  | Impurities: Carbon Monoxide (CO), Carbonyl Sulfide (COS), Hydrogen Sulfide (H2S), Nitrogen (N2), Argon (Ar) | ≤50 ppbv |
|  | Impurities: Ethane (C2H6), Methane (CH4), Water (H2O), | ≤100 ppbv |